# Lecture 8

# Wet Etching

# Current uses:	(	remove damage from whole wafer slices

(	delineate crystal defects

(	planarization by chemical mechanical polishing

(	not for fine features

### Advantages:	(	little substrate damage

(	often highly selective

Disadvantages:	(	Isotropic (usually)	(	undercutting

(	Difficult to control

(	Particle contamination (sometimes)

(	Susceptibility to scum poisoning

Isotropic etch				Anisotropic etch (plasma)

See Handout 5 (Fig. 6.3) for general setup

General chemical features

### Tests for diffusion limitation:	(	weak T dependence of rate

(	more agitation increases rate

See Handout 5 (Fig. 6.5) for example of rxn/diffusion regimes

Mechanisms:  General Features

-	Often incompletely understood

-	May involve intermediates not given in overall stoichiometry

-	Reported etch rates for a system may differ substantially (factors of >2) because of

- difficulty of measuring surface T for fast exothermic rxn

- bubbling

- sensitivity to contaminants/minor products

- sensitivity to surface defects

Examples:

1.	Si

Most based on HF – HNO3 – H2O

2 steps:	(	Si oxidized to SiO2 (natively or by HNO3)

(	SiO2 removed by HF

Overall rxn:

18HF + 4HNO3 + 3Si  (  3H2SiF6 + 4NO(g) + 8H2O

soluble

Notes:	(	intermediate SiO2 not listed!

(	like all etching, this is a redox rxn

is oxidized to SiF6-2	(0 to +4)

NO3– is reduced to NO	(+5 to +2)

formal oxidation state

Rates often shown on a ternary diagram:  See Handout 5 (Fig. 6.4)

Too little HNO3	(	Si not oxidized to SiO2

Too little HF	(	SiO2 not dissolved

Can be either rxn or diffusion limited ( See Handout 5 (Fig. 6.5)

Anisotropic etches

(	Used for Si micromachines (MEMS)

(	Large, electrically isolated devices for high-voltage or radiation-hard applications

Example: 		Si  +  2KOH  +  H2O  (  K2SiO3  +  2H2

Etches [111] directions slower than others because of double

layer:  See Handout 5 (Fig. 6.6).

On Si(100) wafers, get					instead of

Resistivity effects

Heavy n or p doping increases rate for conventional

HF – HNO3 – CH3COOH solution by factor of ~15.

(	Needed for accurate rate predictions

(	Can help delineate heavily doped regions for characterization

(	Can help make very thin films by etching underlying substrate

2. SiO2

Most based on HF–H2O

Overall rxn: SiO2  +  6HF  (  H2SiF6  +  2H2O		No change

in formal

oxid. state.

Mechanism :  very complex

Dilute soln :    3HF (  F–  +  HF2–  +  2H+

active

not active

Concentrated soln :  also get H3F4– or H4F5– complexes

Solutions often buffered with NH4F.

Lecture End ––––

# Text boxes

or CH3COOH,  reduces surface tension ( better wetting, smoother surface

Any step can be rate limiting.  Stirring/agitation can reduce (but not remove diffusion limitation.