# Lecture 9

Review of buffers: Intended mainly to keep pH constant in response to adding acids or bases

Employ weak acids & conjugate bases

HA ( H+  +  A–

H3O+

Ka  =

dissociation constant

Ka is small for a weak acid

Note:

e.g., HF, 25(C

Ka is large for a strong acid

e.g. HCl:	Ka >> 1

Quantitative analysis

1.  What is H+ in a weak acid solution of formal concentration CA?

(  (

not = because of H2O dissociation

Also,

For weak acid, CA is fairly large,

(   (

2.	Calculate pH change when 100 ml of 0.05M HCl is added to 400 ml of a buffer that is 0.2M in HF and 0.3 M in NH4F

=

Starting  pH:   assume

( =  	(

(

Ending

( =  	(

(

(                      Small

In HF / NH4F buffer, however, the purpose is not just to keep pH constand during rxn.  Adding NH4F also affects,  etc.  This is more complex.       See Handout 5

3.	 Metals

Need for removing metallization, leftover metal from silicidation.  Often either acids or bases work.

e.g. Al:

(even H2O would etch Al, except for passivating oxide)

Typical etch is an acid (since base attacks SiO2)

20 parts by vol			CH3COOH

3					HNO3

77					H3PO4

Problems:	-	Metals polycrystalline  ragged edges

-	Remove alloying compounds in Al (e.g. Si)

(leave precipitates behind)

-	Undercutting in multimetal etch with Au or other passive metal on top

See Handout 5:  this is all redox.

(

(

____________________________________

(

Similar analysis for Al, Cr, Co, Ni gives (+) voltage

( will etch in pure acid.

Lecture End ––––

# Text boxes

doesn’t go, must be (+)

don’t change V for 2e–

bubbles

Note:  Both decrease due to distribution