# Lecture 10

# Plasma Etching

### Uses:	(	very fine lines

(	deep trenches

### Advantages:	(	can be very anisotropic

(	easy to control

Disadvantages:	(	selectivity lower than wet etch

(	mechanism very complicated

(	difficult to predict behavior a priori

(	more complex equipment

P=10–4 – 10 torr

Fraction ionized ~10–6

Modes of Operation

- Ion milling (relatively uncommon)

- Use inert gas (Ar) at low P (<10–3 torr), high V

- Etching by physical erosion only

- Anisotropic, poor selectivity

- Considerable damage to substrate

- Reactive ion etching (very common)

- Use reactive F or Cl – containing gas at modest P (10–3 – 10–1 torr), modest V (70 – 300V)

- Etching by nonlinear combination of sputtering and rxn

- Fairly anisotropic, decent selectivity (~25)

- Some damage

- Free radical plasma

- Use reactive F or Cl – containing gas at “hi” P (10–1–10 torr), low V (< 70V)

- Etching by free radical rxns

- Usually isotropic (without sidewall passivation), selectivity good, especially to photoresist, relatively low rate

- Little damage

# Gas Selection

For Si, SiO2, Si3N4, many silicides many metals

( F-based etchants CF4, C2F6, SF6

e.g.:		Si + 4F( ( SiF4(g)

3SiO2 + 4CF3( ( 2CO + 2CO2 + 3SiF4(g)

SiO2 + 2CHF2 ( 2CO + H2 + SiF4(g)

Si3N4 + 12F( ( 3SiF4 + 2N2

Ti + 4F( ( TiF4(g)

For Al (no volatile fluoride ( passivation)

( Cl-based etchants CCl4, BCl3 + Cl2 + CHCl3 + N2, BCl3 + Cl2

e.g.:	Al + 3Cl( ( AlCl3(g)

Problems:	(	cold spots ( AlCl3 condenses

(	expose to H2O ( form HCl (corrosion)

Al2O3 (particles)

(	residual surface Cl ( corrosion of Al

(flush with F species at end)

For photoresist stripping

( O2 – based etchant

Often multiple gases used because:

(	some byproducts deposit passivating layers

(e.g., Photoresist scum) ( add a little O2

(	etchant may react with main substrate but not its surface oxide covering

# A Closer Look at RIE

1.	Physics:	ungrounded plates become negative w.r.t. plasma because e( move further per rf cycle and are depleted from gas phase.

Effect more pronounced when floating (or hot) electrode is smaller than grounded one.

#### Voltage makes ions impinge

at near-normal incidence

(although collisions deflect some)

## Plasma Temperature

Normally T in a gas is characterized by a Boltzmann dist. in velocity u:

In plasmas, there are several distributions:

Ions, e–, neutrals are different, and ions/e– are not Boltzmann!  To get an idea of T, consider a definition based on mean velocity ū:

On this basis,	Tion ~ 400 – 500K

Te- ~ 10,000K (like sun’s surface!)

However, since T is not well defined, standard theories for thermal chemistry don’t apply.

##### Lecture End _____