# Lecture 18

# Thermal Oxidation

Dry oxidation		Si(s) + O2 (g)  (  SiO2 (s)

Wet oxidation		Si(s) + 2H2O(g)  (  SiO2 (g) + 2H2 (g)

Some processes use O2 and H2O

Used for gate dielectric in MOSFETS and field oxide between devices.

# Simplified Deal-Grove Model

In Si oxidation, gas diffusion is always very fast compared to the other steps: gas diffusivities are very high.

1.  Diffusion across oxide limits:

## (in molec/cm2-s)

## Linearizes derivative over entire film.  This is an approximation.

Use Henry’s law (dilute solution in solid) to get Co:

conventional notation.

This implies diffusion is not so fast to destroy equilibrium at interface.

- Reaction at interface limits:  r (molec/cm2-s) = kCi

Put together:

to get Ci

Thus,

molecules O2 /unit vol. SiO2

IC: h(0) = ho

Then solution is:

Let

Then

Two regimes:

- Linear, 			Rxn and diffusion matter

- Parabolic, 	Diffusion dominates

Note:  Both A and B have activation energies:

Thus, for h ( 0,	EA ( ER

h ( (, 	EA ( Ediff / 2

For very small total thicknesses (<30 nm), Deal-Grove model breaks down:  rate is faster than expected.

Nobody knows why.  Campbell’s book shows a “scotch tape” parameterization of  to make the data fit.

Effects of Dopants:

All dopants increase rate.  Some prefer to segregate into oxide.  Campbell’s Fig. 4-16 misleading – has mass balance problems.

impurity in Si

Define segregation coeff.   m = 	––––––––––––

impurity in SiO2

m < 1 (Segregate to oxide)

m > 1 (Segregate to Si)

Slow diffusion in oxide			Fast diffusion in oxide

Lecture End _________

# Text boxes

3 possible rate-limiting steps:

- diffusion through gas film

- diffusion through oxide

- reaction at interface

In principle all 3 can contribute.