Lecture 19

# Si Production

Process flow: (From H. Lee’s book, Fundamentals of Microelectronic Processing)

HCl

# Polycrystalline

electronic grade

Si

1. Molten furnace

Reduce SiO2 (as sand or quartzite) with carbon

CO, SiO, H2O						SiO2, coal, wood chips

|  | Carbon Electrode |  |  |  |
| --- | --- | --- | --- | --- |
| Condense most SiO SiO(g) + CO(g) SiO2 + C |  |  |  |  |
| Form SiC |  | SiO(g)+2CSiC+CO(g) |  |  |
| SiO2 + 2SiC 3Si + 2CO(g) 2SiO2 SiC 3SiO(g) + CO(g) |  |  |
| Si (~2% total O, Fe, Al, Ti) |

2. Fluidized bed

Principal reaction is:		Si + 3HCl  SiHCl3 + H2

But there are others.

3. Separation & purification

Done by distillation.  It’s easier to purify gases than liquids or

solids.

4. Electronic grade Si production

Most is made in a Siemens reactor

SiHCl3  + H2  Si + mostly HCl ( + some SiCl4)

But:	1.	Slow batch process (low

rate, not continuous)

2.	High loss of SiCl4

3.	High power consumption

Hemlock Semiconductors Corp. calls this deposition “CVD”

They break up Si into uniform size by hand with Ti hammers!

Some work is in fluidized beds now, as in next example.

Quantitative Treatment of Fluidized Bed Reactor

This example is a fairly sophisticated use of mass balances.

Provides experience with:

( Distribution functions

( Converting difference equations into differential equations

Let p(r) be a distribution

fxn describing probability

of having size r

Assume:	(	well-mixed CSTR  pout  = pbed

(	constant solid density

(	no attrition

(	constant deposition rate (cm/s)

(	steady state

Physical picture:	T & P of reactor set .  Solid feed picks up mass from gas phase before exiting.

Question:	Given Fin and pin(r), what is Fout and pout(r)?

(To get an answer simply, we have to assume there is some parameterization for pgas in terms of pout.)

Approach:	Since we need the size distribution as a function of r, we need a differential mass balance on particles between r and r + (r.

Up to now we have done only integral balances, yielding algebraic equations, because we haven’t needed to know what’s going on inside the control volume.

Now we need knowledge about the size distribution inside the control volume.  This leads to differential equations.

Our control volume will not be fixed in space, but will be a size range within the distribution between r and r + (r.

General form:  accum = in – out + gen – cons	Do for particles between r and r + (r

solid product		gas stream

So   0	=	solid inflow	–	    outflow		–	   outflow

steady

state		entrance by		exit by growth	    growth of particles

+	growth at r	–	  at r + (r		+   staying within

(all in g/s)

(1)

another view of this term:

Let 	Then  W(beddr  gives the weight at r.

Dividing by  dt  gives the rate of change

What about the generation term?  Let N(r) = number of particles between r and r + (r

Then gen = 	where

and N(r) comes from

So 		gen  		since pout = pbed.

Substituting into (1) and dividing by (r,

Let (r ( 0, ignore Fgas (assume no entrainment), divide by

(

We’ll solve this equation next time.

Lecture End ––––

# Text boxes

Sand

Arc Furnace (molten)

Fluidized bed

Separator

Fluidized bed or decomp. chamber

Metallurgical grade Si

~ 0.3% Fe

~ 0.1% Al

~ 0.1% Ca

many others

Purified

SiH4, SiHxCl4-x

SiH4,

SiHxCl4-x

cm3/particle

1600oC

1780OC