Lecture 24

# Ion Implantation

( Shoot ions into substrate, then anneal to activate and remove

damage.

( Projected range depends on implant energy.  Now implanters

operate at 500V or less for ranges < 20 nm.

( This is the main way dopants are now introduced in critical

applications (sources, drains).

( Method is especially useful for forming shallow junctions with

high doping levels.

Advantages:

( High speed

( Excellent reproducibility and controllability

( Ability to attain dopant levels higher than the solid solubility limit

Disadvantages:

( High expense for implanter (a fancy, high-output mass

spectrometer)

( Implantation damage must be annealed out.  We’ll treat this later.

( Can get ion channeling along high symmetry directions.  Fix by

preamorphizing implant with Ge.  But this introduces new

complications.

1. Implantation issues

Diagram of implanter

( Implantation species typically BF3 (F remains in substrate) or AsH3

( Maximum concentration is below surface

Diagram of concentration vs. depth, lateral position

2.  Annealing issues

( Process done almost exclusively by RTP  (usually called RTA:

rapid thermal annealing)

( Spike anneal to 1050(C for a few seconds typically used.

( Ramp up at 75–500(C/s, limited by lamp density and control

issues

( Ramp down at 75(C/s or less, limited by radiative cooling

( Recipe reduces transient enhanced diffusion: the initial extremely

rapid spreading of dopants by defect-mediated diffusion.  TED

limits shallowness of the junction, particularly for boron.

3. Limiting TED

- Complexity of the diffusion-reaction equations

See Text Handout – Point out:

( the many reactions involved

( the need for full-blown transient 3-D PDE’s (although we

simulated only 1-D for computational efficiency.

( the complications introduced by charged species and Poisson’s

eqn.

( effects of surface space charge (end of text)

- Nonthermal illumination effects

See Handout

Lecture End ––––